## Slide 1: Utilization of the critic subnetwork of a generative adversarial network as detector of morphological material change in image data
Ariana Beste/7555
Dan Bolintineanu/1516, Dan Bufford/7555
FY22 Exploratory Express LDRD, Project 226346
SAND2022-9134 C

## Slide 2: Problem
Surveillance
Traditional morphology analysis
Segmentation
Dimensionality Reduction
Single-point metrics
Spatial correlations
Regional statistics
A priori choice
Information loss
Dependence on experimental setup
Original images
Representation of complex function
Computer Vision
Convolutional neural network
No prior choice
Little information loss
Reduced dependence on experimental setup
Lack of test data

## Slide 3: Algorithmic Approach
Wasserstein Generative Adversarial Network (WGAN)
Critic
Generator
1 Hsu, T., et al., Microstructure Generation via Generative Adversarial Network for Heterogeneous, Topologically Complex 3D Materials. Jom, 2020
Utilization of previous implementation1 to generate realistic microstructures from SEM images
Critic
Scores generated images according to how well they resemble the training images
Generator
Generates synthetic images that resemble training images as closely as possible
Critic and generator trained together with images of pristine material
Critic tested with images of potentially altered material morphology -> Image scores
Generator
3 up-sampling/convolutional (ReLu)/batch normalization layers, 1 convolutional (Tanh) layer
Filters 256-128-64-32
Critic
7 convolutional layers (LeakyReLu)
Filters 32-32-64-64-128-128-256

## Slide 4: Data
CT scan of pristine Pharmatose
1800 2d images
Each 2d image 2,000x2,000 pixels
Batch: 64 down-sampled (1/4) 512x512 cropped segments
Training
HMX microstructure generation with single 3,000x3,000 pixel SEM image 1
Testing
Image Transformations
Varying Particle Sizes
Aged Material (120°C)
Pristine
1 Week
2 Weeks
1 Chun, S., et al., Deep learning for synthetic microstructure generation in a materials-by-design framework for heterogeneous energetic materials. Scientific Reports, 2020. 10(1).
Swirl
Polar
Wave
Large
Medium
Small

## Slide 5: Results – Image Generation
Critic scores (1000 images)
Real
Image 440
Epoch 800
Epoch 700
Epoch 600
For a given epoch, the critic scores real and fake images similarly
Scores vary significantly between epochs
“Blobs” in fake images don’t seem to improve
Training restriction 512x512 pixels image size

## Slide 6: Results – Image Generation
100 images
Converging?
Critic scores (1000 images)
Count
Count
Count
Voxel -1
Volume fraction: epoch 800 closest to real images
Interfacial line length: different epochs similar distribution
Despite “blobs” image properties appear to be well reproduced
100 images

## Slide 7: Results – Scores for transformed images
100 images
Critic scores (1000 images, critic epoch 800)
Count
Count
Voxel -1
Although there is some response, critic is not sensitive enough to pick up differences in particle shape
Swirl
Polar
Wave
Count
Two-point correlation function Example image, polar transformation
Pristine
100 images

## Slide 8: Results – Scores for varying particle sizes
100 images
Critic scores (1000 images, critic epoch 800)
Count
Count
Count
Voxel -1
Critic scores images of different particle sizes differently and in consistent order
Pristine
Large
Medium
Small
100 images

## Slide 9: Results – Scores for aged data
100 images
Count
Voxel -1
Unlikely, that critic scores can differentiate between materials …
Count
Network training in progress
Scores will be available soon
Pristine
1 week
2 weeks
Only subtle differences between pristine and aged material using traditional metrics.
100 images

## Slide 10: Conclusions
Concept works, the critic of a GAN can be used as a detector of morphological change but significant improvements needed before the critic can be used in practice:
Image generation without “blobs”
Increase critic sensitivity
Increase of training image size
Help (ideas, collaborations) from ML/DL community very much appreciated
Potentially interested customers: NA-193, Aging & Lifetimes