## Slide 1: Building a new generation of multiscale materials models with machine-learned interatomic potentials
Megan McCarthy, Department 1444 – Computational Multiscale
Mitchell Wood 1444, Aidan Thompson, 1444
Funding: DOE, Office of Science, Fusion Energy Sciences
SAND2022-8952 C

## Slide 2: What are interatomic potentials? Why add machine learning?

## Slide 3
Physical models of materials are constrained to limited length- and time-scale regimes.
Solid Mechanics, Hydrodynamics
Kinetic Monte Carlo, Phase Field
Time
Length
ps
ns
µs
ms
pm
nm
µm
mm
Electronic Atomic Meso Continuum
Atomistic Molecular Dynamics
Electronic Structure

## Slide 4
Input: ion (atom) positions, pseudopotential
Output: electronic structure, energy, forces, stress
Immense predictive power
Expensive
O(N^3) scaling
N ~ 100s-1000s
Quantum Simulations
Input: atom positions, interatomic potential
Output: energy, forces, stress
O(N) scaling
N ~ millions, billions
Accuracy is a problem
Classical Molecular Dynamics
Machine-Learned Interatomic Potential (MLIAP)
Energyi = U(features)
Ground truth
Reduced order model
Quantum accuracy is critical in modern materials modeling, but is limited in system sizes and times.
Time
Length
ps
ns
µs
pm
nm
µm
Electronic Atomic Meso
Atomistic Molecular Dynamics
Electronic Structure

## Slide 5
Time
Length
ps
ns
µs
pm
nm
µm
Electronic Atomic Meso
Atomistic Molecular Dynamics
Electronic Structure
Input: ion (atom) positions, pseudopotential
Output: electronic structure, energy, forces, stress
Immense predictive power
Expensive
O(N^3) scaling
N ~ 100s-1000s
Quantum Simulations
Input: atom positions, interatomic potential
Output: energy, forces, stress
O(N) scaling
N ~ millions, billions
Accuracy is a problem
Classical Molecular Dynamics
Machine-Learned Interatomic Potential (MLIAP)
Energyi = U(features)
Ground truth
Reduced order model
Molecular dynamics (MD) codes can simulate much larger systems, but traditional interatomic potentials limit accuracy.

## Slide 6
Time
Length
ps
ns
µs
pm
nm
µm
Electronic Atomic Meso
Atomistic Molecular Dynamics
 Model, model evaluation
Electronic Structure
 Training
Input: ion (atom) positions, pseudopotential
Output: electronic structure, energy, forces, stress
Immense predictive power
Expensive
O(N^3) scaling
N ~ 100s-1000s
Quantum Simulations
Input: atom positions, interatomic potential
Output: energy, forces, stress
O(N) scaling
N ~ millions, billions
Accuracy is a problem
Classical Molecular Dynamics
Machine-Learned Interatomic Potential (MLIAP)
Energyi = U(features)
Ground truth
Reduced order model
Machine learning is being used to successfully bridge quantum- and atomic-scale modeling and simulation.

## Slide 7: MLIAPs can be developed with a variety of descriptors and ML methods.
Hyperparameter
Optimization
(Single Objective GA)
https://github.com/FitSNAP/FitSNAP
Ground truth
energies,
forces,
stresses
(DFT = Density Functional Theory)
Spectral Neighbor Analysis
Creates a Spectral Neighbor Analysis Potential (SNAP)
Outputs energy and force errors
Sets up for material property and/or hyperparameter optimization (often, SOGA objective functions)
Adjusts hyperparameters based on objective functions
Optimization loop
Individual material model (MLIAP)
Thompson et al. J. Comp. Phys. 285 2015

## Slide 8: FitSNAP is designed to give the user flexibility in model and descriptor choice.
https://github.com/FitSNAP/FitSNAP
Polynomial models
DFT Training
Set of Descriptors
Weights
Regularization
Penalty
Linear SNAP, Quadratic SNAP
Wood & Thompson, J Chem Phys 148, 2018
Neural network models
D. de Oca Zapiain, arXiv:2201.09829v2
Explicit Multi-Element (EME) SNAP
Cusentino, Wood, Thompson, JoPC 147, 2020
EME
Linear
Weighted RSME
In progress: ‘ChEmbedded’ SNAP
Tunes accuracy/speed between linear/EME SNAP
L. Lopes, N. Lubbers (LANL)
Atomic Cluster Expansion (ACE)
Lysogorskiy et al., npj 7, 2021

## Slide 9: MLIAPs enable us to run extremely accurate MD simulations at previously-impossible length and time scales!
SNAP carbon:
Simulations with billions of atoms!
New insights into physics of phase changes and deformation mechanics
Extremely computationally efficient - SNAP on Summit (GPUs), Gordon Bell Finalist 2021
From USF, Sandia, NERSC, NVIDIA, KTH: K. Nguyen-Cong, J. Willman, S. Moore, A. Belonoshko, R. Gayatri, E. Weinberg, M. Wood, A. Thompson, I. Oleynik
doi.org/10.1145/3458817.3487400

## Slide 10: A (non-exhaustive) list of SNAP MLIAPs in use
-
-
2022
-
-
https://github.com/FitSNAP/FitSNAP
MoNbTaTi
HEA alloy design
-
>5,000
GeSe
Vitrification
-
>5,000
EME
W
Model form selection
-
330,000
NN
LiMoS
Li-ion batteries
-
>5,000
-
SiGeSnPb
Thermoelectric materials
-
>5,000
-
SNL Involved, Independent
Ta
System
InP
WBeHe
Actinides
NiMo
LiN
Various
InP
Al
2014
Year
2015
2017
2018
2018
2019
2020
2020
2021
Mo
2017
Fe
2021
AlNbTi
2020
Si
2020
Dislocation motion
Usage
Radiation damage, defects
Plasma facing materials
Shock, phase transitions
Phase diagram prediction
Super-Ionic Conductor
Accuracy/Cost comparison
Radiation damage, defects
Predicting electron density
Phase diagram prediction
Magnetic phase transition
High entropy alloy design
Neural network SNAP
31
NDoF
31
56
56
31
31
10-130
241
91
363
NTraining
665
25,052
20,000
2,000
3,000
1,000
1,000
30
Linear
Descriptors
Linear
Linear
Quadratic
Linear
Lin+Charge
Lin, Quad
EME
NN
SNL, Thompson
Origin
SNL, Thompson
SNL, Wood
SNL/LLNL
UCSD, Ong
UCSD, Ong
UCSD/SNL
SNL, Cusentino
SNL, Ellis
31
1000
Linear
UCSD, Ong
1596
683
Quad+Spin
SNL, Nikolov
1596
7,250
Quadratic
SNL, Tranchida
1596
>5,000
NN
UNLV, Zhu
9
W
2022
Model form selection
-
330,000
NN
LANL/SNL

## Slide 11: The trouble with (atomistic) training sets … and some solutions!

## Slide 12: Creating and curating MLIAP training sets is one of the field’s biggest challenges.
https://github.com/FitSNAP/FitSNAP
Bulk crystal
Interfaces
Liquids
W
Zr
C
Hand-crafted training sets
Up to now:
Curated training sets created by hand from scratch, using physical intuition
Pros: Works very well with targeted (i.e., limited) materials systems and specific conditions, experts + physical intuition can spot model failures well
Cons: transferability, not easy to automate (initial training + retraining), need expert(s)
E. Sikorski (SNL 1444)
Automation is needed! Two approaches in the pipeline:
Active learning with uncertainty quantification
Automated training set generation using ‘max entropy’ approach

## Slide 13: Experts can observe and correct model errors using physical intuition (‘active learning’), but it is time-consuming.
https://github.com/FitSNAP/FitSNAP
Hands-on route:
Run MD
Carve out structures
Run quantum simulations
Re-Train ML-IAP
How can we get our software to automatically recognize model failures?

## Slide 14: Active learning paired with uncertainty quantification can improve MLIAP training efficiency.
https://github.com/FitSNAP/FitSNAP
Pool-based, uncertainty-informed AL paradigm
Structures with high predictive uncertainty added here provide a large improvement in accuracy
L. Williams (SNL 8351)
K. Sargsyan (SNL 8351)
H. Najm (SNL 8300)
Implementation
Hands-on route:
Run MD
Carve out structures
Re-Train ML-IAP
Run quantum simulations
(run quantum simulations)
How can we get our software to automatically recognize model failures?

## Slide 15: ‘Bad structures’ can be very effective in making MLIAP performance more robust.
https://github.com/FitSNAP/FitSNAP
Physics-based or model failure, hand-selected
Physics-based, “physically improbable,” semi-automated
E. Sikorski (SNL 1444)
USPEX
A. Oganov et al., J. Chem. Phys. 124, 2006

## Slide 16: Emphasizing descriptor diversity over physical ‘correctness’ can benefit training sets/MLIAPs.
https://github.com/FitSNAP/FitSNAP
‘Bad structures’ increase descriptor diversity!
Physics-based or model failure, hand-selected
Physics-based, “physically improbable,” semi-automated
E. Sikorski (SNL 1444)
USPEX
A. Oganov et al., J. Chem. Phys. 124, 2006
 Fewer extrapolations, more interpolations
D. de Oca Zapiain (SNL 1864), M. Wood (SNL 1444), C. Pereyra (UC Davis), N. Lubbers (LANL), D. Perez (LANL), A. Thompson (SNL 1444)
arXiv:2201.09829v2
Under review:

## Slide 17: Emphasizing descriptor diversity over physical ‘correctness’ can benefit training sets/MLIAPs.
https://github.com/FitSNAP/FitSNAP
D. de Oca Zapiain (SNL 1864), M. Wood (SNL 1444), C. Pereyra (UC Davis), N. Lubbers (LANL), D. Perez (LANL), A. Thompson (SNL 1444)
arXiv:2201.09829v2
Karabin and Perez, JCP 153, 2020
‘Bad structures’ increase descriptor diversity!
Physics-based or model failure, hand-selected
Physics-based, “physically improbable,” semi-automated
E. Sikorski (SNL 1444)
USPEX
A. Oganov et al., J. Chem. Phys. 124, 2006
Under review:
 Fewer extrapolations, more interpolations
Descriptor-based structure generation: entropy maximization

## Slide 18: Entropy maximation methods can be used to generate an entire training set from scratch.
https://github.com/FitSNAP/FitSNAP
Karabin and Perez, JCP 153, 2020
‘Bad structures’ increase descriptor diversity!
Physics-based or model failure, hand-selected
Physics-based, “physically improbable,” semi-automated
E. Sikorski (SNL 1444)
USPEX
A. Oganov et al., J. Chem. Phys. 124, 2006
Entropy maximization training set generation: ‘ignores’ physics (less human bias), fully automated, can be used to generate training data for any ML model (works in descriptor space)
Descriptor-based structure generation: entropy maximization
 Fewer extrapolations, more interpolations
D. de Oca Zapiain (SNL 1864), M. Wood (SNL 1444), C. Pereyra (UC Davis), N. Lubbers (LANL), D. Perez (LANL), A. Thompson (SNL 1444)
arXiv:2201.09829v2
Under review:

## Slide 19: Conclusion
https://github.com/FitSNAP/FitSNAP
Machine-learned interatomic potentials (MLIAPs) allow us to build very accurate and fast-running materials models to explore nanoscale phenomena!
Augmenting MLIAP development with active learning and automated training set generation increases model development throughput, allowing us to do more cool science more quickly!
Contact: megmcca@sandia.gov

## Slide 20
https://github.com/FitSNAP/FitSNAP

## Slide 21: Abstract
Building a new generation of multiscale materials models with machine-learned interatomic potentials
Excellent physical models exist to simulate material behavior at specific length and time scales. However, many challenges still remain in linking materials behavior across scales. Applying the techniques of machine learning to the issue of multiscale simulation has led to a revolution in atomistic materials modeling. Machine-learned interatomic potentials (MLIAPs) connect extremely accurate but computationally expensive quantum modeling techniques with lower fidelity but fast classical molecular dynamics (MD) models. In other words, MLIAPs allow MD simulations to achieve quantum accuracy at unprecedented system sizes and time scales. The diversity of model forms and feature sets for MLIAPs, paired with popular MD codes such as LAMMPS, has also opened new pathways to accelerating MLIAP development. These developments have enabled significant progress to be made in challenging scientific and engineering areas, including modeling conditions inside future fusion reactors, understanding magnetic materials in extreme environments, and accelerated exploration of complex alloy systems.
Though MLIAPs represent a new paradigm in the atomistic modeling community, the traditional problems in ML/DL regarding retaining accuracy while extrapolating remain. This talk will overview our group’s strategies to address these issues using the open-source and user-friendly FitSNAP MLIAP generation code. We will explore how current implementations of active learning, uncertainty quantification, and automated training set generation are systematically improving MLIAP simulation accuracy and extrapolative capabilities.